Introduction

Currently the major goals in the area of space electronics for NASA are to make them ever smaller and radiation-hard.  Currently, space electronics are based on silicon, but unfortunately, silicon is not radiation hard.  Due to their nanometer-scale size, purported stability, well-documented high conductivity and Young's modulus, carbon nanotubes may be ideally suited to applications in space electronics.  Hence, the purpose of this project is to examine the effect of ionized radiation on the mechanical and electronic properties of carbon nanotubes and determine their suitability to space applications.  Results from samples grown at the University of Michigan in an inductively coupled plasma (ICP) system, CNTs produced at NASA and

Tubes@ Rice which are known single-walled carbon nanotubes, will be compared in this paper.

Methods

The carbon nanostructures were produced at the University of Michigan by placing a Si wafer onto which 10-20 nm of Fe were laser ablated, inside the ICP system for approximately five and a half hours. The plasma contained 87% Argon, 6.5% Methane and 6.5% Hydrogen.  The carbon nanotubes from NASA were produced using the DC arc-discharge method and cleaned using the cleaning process developed by Dr. Benavides.  Tubes@Rice, which are single-walled carbon nanotubes are from Rice University.  They were produced by Dr. Smalley’s group via laser vaporization of graphite as described in their 1995 paper
.

These samples have thus far been examined prior to radiation using Transmission Electron Microscopy (TEM) and micro-Raman Spectroscopy (at 514.5 nm).    For Transmission Electron microscopy, a Hitachi-800 Transmission Electron Microscope (200 KeV, .00251 nm wavelength) was used.  The Micro-Raman system was consists of an Argon-ion laser, monochromator, photo-multiplier tube (PMT) and optical microscope set-up in back-scattered configuration 

Results

[image: image1.png]



Figure 1: Carbon nanotubes grown at NASA Goddard Space Flight Center

(DC-arc discharge method, bar = 400 nm)

[image: image2.emf]A:\A0481302.1

Pk=Gauss Amp  1 Peaks  Bg=Linear

r

2

=0.978671  SE=102.793  F=1101.24

1.5679e+06

1.5e+06 1.52e+06 1.54e+06 1.56e+06 1.58e+06 1.6e+06

Raman Shift (cm

-1

)

0

500

1000

1500

2000

2500

Intensity (a.u.)

0

500

1000

1500

2000

2500

Intensity (a.u.)


Figure 2: Raman of NASA sample A04 in Tangential mode region @ 514.5 nm deconvoluted using PeakFit with Gaussian Peak Amplitudes

[image: image3.emf]A:\A0673002.1

Pk=Gauss Amp  3 Peaks  Bg=Linear

r

2

=0.238647  SE=18.6777  F=2.82106

1.5092e+06

1.5243e+06

1.5419e+06

1.5e+06 1.52e+06 1.54e+06 1.56e+06 1.58e+06 1.6e+06

Raman Shift (cm 

-1

)

-25

0

25

50

75

100

Intensity (a.u.)

-25

0

25

50

75

100

Intensity (a.u.)


Figure 3: Raman of NASA sample A06 in Tangential mode region @ 514.5 nm deconvoluted using PeakFit with Gaussian Peak Amplitudes

[image: image4.emf]A:\A0773002.1

Pk=Gauss Amp  3 Peaks  Bg=Constant

r

2

=0.781562  SE=15.507  F=36.1772

1.5221e+06

1.5424e+06

1.5955e+06

1.5e+06 1.52e+06 1.54e+06 1.56e+06 1.58e+06 1.6e+06

Raman Shift (cm 

-1

)

0

10

20

30

40

50

60

70

80

Intensity (a.u.)

0

10

20

30

40

50

60

70

80

Intensity (a.u.)


Figure 4: Raman of NASA sample A07 in Tangential mode region @ 514.5 nm
[image: image5.png]



Figure 5: TEM of single carbon nanostructure grown in ICP system (bar = 40 nm)

[image: image6.jpg]



Figure 6: TEM of lower portion of the above carbon nanostructure (bar = 25 nm)

[image: image7.emf]A:\BUM3701C.1

Pk=Lorentz Amp  11 Peaks  Bg=Linear

r

2

=0.666412  SE=34.8953  F=5.05303

1.5352e+06

1.5469e+06

1.5693e+06

1.5729e+06

1.5816e+06

1.5931e+06

1.6113e+06

1.6127e+06

1.6201e+06

1.6317e+06

1.6392e+06

1.525e+06 1.55e+06 1.575e+06 1.6e+06 1.625e+06 1.65e+06

0

11.111

22.222

33.333

44.444

55.556

66.667

77.778

88.889

100

0

11.111

22.222

33.333

44.444

55.556

66.667

77.778

88.889

100


Figure 7: Raman of wafer containing carbon nanostructures above in Tangential mode region @ 514.5 nm deconvoluted using PeakFit with Lorentzian peak amplitudes
[image: image8.png]



Figure 8: TEM of Tubes@Rice (bar = 40 nm)

[image: image9.emf]Raman of Tubes at Rice at 514.5 nm

0

500

1000

1500

2000

2500

3000

3500

4000

2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06 2E+06

Raman Shift (cm^-1)

Intensity (a.u.)

Intensity (a.u.)


Figure 9: Raman of Tubes@Rice in the Tangential Mode Region at 514.5 nm

[image: image10.emf]A:\Bucky Paper\TM-G\Buckey710.   

Pk=Lorentz Amp  11 Peaks  Bg=Linear

r

2

=0.973273  SE=84.064  F=284.894

1.5114e+06

1.5261e+06

1.5421e+06

1.5545e+06

1.5617e+06

1.5672e+06

1.5856e+06

1.595e+06

1.6235e+06

1.6355e+06

1.6425e+06

1.5e+06 1.55e+06 1.6e+06 1.65e+06

0

250

500

750

1000

1250

1500

1750

2000

0

250

500

750

1000

1250

1500

1750

2000


Figure 10: Raman of Tubes@Rice deconvoluted using PeakFit with Lorentzian Peak Amplitudes
Discussion and Future Work

Currently, as can be seen by comparing the Raman results (prior to exposure to radiation) of the NASA samples with that of Tubes@Rice, while the NASA samples show promise, whether they are single or multi-walled carbon nanotubes cannot be determined at the 514 nm wavelength.   These samples clearly need to be examined at the 633 nm wavelength with a Helium-Neon laser, which provides for better coupling and examination of the radial breathing modes.  The TEM micrographs provide some insight into the average dimensions of the nanotubes as well as to their crystallinity.  However, whether the CNTs are multi-walled or single-walled must be determined using HR-TEM.  Also, the irradiation of the NASA samples, Tubes@Rice and the samples grown with ICP at the University of Michigan, is expected to be done early this year.

Acknowledgements

Many thanks are owed to the following people:

Dr. Jeannette Benavides of the NASA Goddard Space Flight Center, who generously donated her time, provided excellent guidance, and stepped me through her cleaning process.

Mr. Harry Shaw, my mentor, of the NASA Goddard Space Flight Center who provided sound advice at various junctures in this project.

Ms. Shavesha Anderson of the NASA Goddard Space Flight Center, who taught me how to use the carbon arc welder and other equipment, and introduced me to other people at the center who were very helpful.

Mr. Fred Felt of the NASA Goddard Space Flight Center, who taught me how to use the StereoScan 38FE scanning electron microscope.

Dr. Reginald Ronningen and Dr. Al Zeller, whom in the coming months will be operating the ion source and irradiating the carbon nanotubes and have already given a significant amount of time to this project.

Dr. Virginia Ayres, my major professor, who generously shared her time and expertise in SPM portion of the project

Last but not least, Dr. Martin Crimp, associate professor in the ChEMSM Department at Michigan State University, who generously donated his time as well as “microscope time” on his TEM 

Effects of Ionized Radiation on the Mechanical and Electronic

Properties of Carbon Nanotubes

Summer 2002 JPFP Mini-Grant Project Report

By: Susan Song

A tangential breathing mode for single-walled carbon nanotubes





No tangential breathing mode was detected





No tangential breathing mode was detected





A tangential breathing mode for single-walled carbon nanotubes





A tangential breathing mode for multi-walled carbon nanotubes





A tangential breathing mode for single-walled carbon nanotubes





A tangential breathing mode for single-walled carbon nanotubes








� "Catalytic Growth of Single-Walled Nanotubes by Laser Vaporization." T. Guo, P. Nikolaev, A. Thess, D. T. Colbert and R. E. Smalley. Chemical Physics Letters, 243, 49-54 (1995).








