1. Scope and Purpose

This document addresses the configuration variables which have been found to affect Ball Grid Array (BGA) interconnect reliability.  Preferred configurations which control these variables and enhance the BGA’s interconnect reliability are discussed.  Examples of these configuration variables are provided in Appendix A.  Commercially available analysis tools are discussed which can be used to assess the reliability of a BGA interconnect based on its configuration variables.

This document is limited to a discussion of BGA’s and does not investigate Column Grid Array packages.  It is also limited to interconnections between BGA’s and polymeric printed circuit boards (PCBs).

2. BGA Reliability

BGA solder joint reliability is normally characterized by thermal cycle life.  CTE mismatch between the part and the PCB as well as mechanical stress due mechanical bending or board warp are the leading environmental contributors to failure. Typical lifetimes for BGA joints are between 100 thermal cycles and ~6000 thermal cycles for temperature excursions between -55°C and 100°C.  Life expectancy will be shorter for greater temperature swings.

A large number of variables related to the physical design of a BGA package, the layout pattern on the PCB and the application of solder to the PCB prior to solder reflow will affect the thermal cycle life of the final BGA joints.  These variables are discussed in the following sections.

3. Package Material:  Plastic vs Ceramic

Reliability studies have shown that Plastic BGAs (PBGA) have longer lived solder joints that those of Ceramic Ball Grid Array (CBGA) joints.  The reasons include better Coefficient of Thermal Expansion (CTE) match and coplanarity is less of an issue.  Thermal cycling ranges beyond 20oC to 85oC will further reduce CBGA joints.  PBGAs should be selected if the application allows it.

Ceramic packages, largely manufactured for the high reliability market or where thermal management necessitates a high conductivity package material, have not been manufactured often as Ball Grid Arrays.  Instead, column interconnects are being offered to increase pin count for ceramic packages.  Column Grid Array reliability is not treated herein.

3.1. Coefficient of Thermal Expansion Matching

For a PBGA, the selection of the PCB laminate system is not critical since both FR-4 and polyimide have a CTE closely matched to Bismaleimide-Triazine (BT), which is usually the internal package substrate material. Ceramic BGA’s have a CTE mismatch with all typical PCB laminates.  For applications where large thermal excursions are expected an FR-4 with high glass transition temperature should be used.  Typical thermal coefficients of expansion are shown in Table 1 for the various materials involved.

| #### Table 1 Typical Coefficients of Thermal Expansion |  |  |
| --- | --- | --- |
| Material | CTE (x-y axis)ppm/oC | CTE (z axis) ppm/oC |
| Tin-lead solder | 24 | 24 |
| Copper | 16-18 | 16-18 |
| FR-4 | 16-18 | 60-85 |
| Polyimide | 15-18 | 65 |
| BT | 15 | 50 |
| Epoxy Overmold | 15 | 15 |
| Silicon | ~2.6 | ~2.6 |
| Alumina oxide | 3-6 | 3-6 |

4. Package Size vs Die Size

The BT package substrate in a PBGA package is organic giving it a CTE closer to that of the laminate polymeric PCB than that of the die itself.  Therefore, the larger the die the more pronounced the effect of the CTE will be and the less reliable the interconnect.  A very large die and a large package will be more sensitive to board warp and mechanical effects associated with uneven thermal conditions (such as during reflow), shock and vibration.

5. Ball Size to BGA Pad Size

BGA’s with larger solder balls tend to have higher reliability than smaller balls.  The larger solder balls provide greater standoff and more mechanical compliance.  The greater solder mass of the larger balls provides better thermal conductivity.  Extremely small balls are used to increase interconnect density which introduce a greater opportunity for electrical shorting between contacts and more sensitivity to thermal design issues.

6. Die to Substrate Connection

The three common methods of electrically connecting the die to the package are wire bond, flip chip, and tape automated bonding. Of these three, wire bonded devices are more reliable because the interconnections have stress relief. Wire bonded devices should be selected if available.

7. Moisture Sensitivity

PBGA’s have not been shown to be any more sensitive to moisture than their leaded, plastic counterparts.  All protections and practices associated with plastic encapsulated microcircuits (PEMs) for space hardware also apply to PBGA packages.  Parts with moisture sensitivity levels 1 and 2 per J-STD-033A are recommended.

8. Substrate and PCB Pad Configurations

On both PCB’s and the package’s substrate, there are two primary pad configurations for BGA solder ball attach:  Solder Mask Defined (SMD) and Non-Solder Mask Defined (NSMD).  SMD pads allow the solder mask to touch the pad.  NSMD pads limit the solder mask to outside of the pad area, (Figure 1). With SMD pads, a smaller ball to pad interface is achieved resulting in a less robust connection. Also, it has been shown that the sharp edges of the solder mask in SMD pads can initiate solder joint cracking at the ball to pad interface. When available, devices with NSMD substrate pads should be chosen.  PCB layout should always use NSMD pad design for BGAs.  The manufacturer’s recommended pad size should be used.

Package substrate

Printed wiring board

Solder mask defined pad

Non-solder mask defined pad

Solder mask defined pads

Figure 1, SMD vs. NSMD

9. PCB Design Considerations

BGA package interconnect reliability is highly dependant on the unit as integrated with the PCB and the overall mechanical and thermal design at the box level.  Pad design, part arrangements across the entire board, via design and trace management are all factors.  The following paragraphs discuss these factors.

9.1 Via Design

Where PCB space is available, the preferred via is an open interstitial via with an aspect ratio of 4:1 or less. The drilled hole size should be 0.020” or larger when possible. The solder mask (SM) opening should provided 0.0015” clearance around the pad.  A minimum of 0.010” of SM between a BGA pad and its via is necessary.  In all cases, vias must be sufficiently isolated from BGA solder pads to prevent solder joint starving.  This can be accomplished by applying solder mask over bare copper to cover the via.  It is preferable to first fill the via with a suitable via filler material before applying solder mask for isolation.   If the pitch of the BGA chosen will not allow these aspect ratio and SM recommendations to be met, then filled vias should be used.   The fill material should be a thermally matched conductive material with or without overplating.

9.2 Part Placement

To facilitate removal and replacement, adequate free space is required around the BGA package. A clearance of 0.125” minimum should be allowed for this.  Careful consideration must be given to the placement of heavy or large thermal mass parts to avoid uneven solder joint reflow or excessive board displacement near the BGA connection during shock and vibration events.

9.3 Routing and Separation

The very dense contact spacing of the BGA package allows significant board size reduction. It is recommended that relatively large traces and spacing be maintained away from the part to enhance PCB production cost and yield.  Traces should be a minimum of 0.004” wide provided this is adequate for the anticipated current.  Traces should be separated by a minimum of 0.004” provided this is adequate dielectric separation for the application.

9.4. Stencil Design/Type

The main considerations for the stencil design should be solder paste volume, aperture shape, aperture size and printing quality.  Stencils are generally electroformed nickel or stainless steel which is laser cut or precision etched.  Precision etching can be used for component pitches down to 0.635mm (0.025”) and laser cut for component pitches below this.  The stencils are generally in the 0.004” to 0.008” thickness range. A 1.5o – 2.5o draft angle of a trapezoidal aperture offers the best paste release characteristics and deposits that are resistant to slump. Nickel electroforming offers a harder finish than stainless steel and naturally smooth walls to enhance paste release.

9.5 Underfill

Non-reworkable underfill with an epoxy material may be necessary to improve solder joint life. Reworkable underfill is available but test data indicates that it may actually decrease solder joint life so its use is not recommended. For applications where outgassing and offgassing are a consideration, the underfill should be a type that can pass the total mass loss and condensable volatile materials tests prescribed in ASTM E-595 and the criteria established by SP-R-0022A.

9.6. Coplanarity

Generally, the coplanarity of the BGA is very small since there are no leads to bend and the plane of the solder bumps is flat.  The warp of the printed circuit board will generally dictate the coplanarity of the BGA assembly.  It is recommended that the allowable warp of a PCB for BGA use be held to less than 1%; 1% warp could be greater than 0.010 inch under a 35 mm square BGA.  An allowable PCB warp of 0.5% max is recommended.

10. Quality Control and Inspection Techniques

Even though the BGA package and board layout may be theoretically optimized for reliability by design, the process of manufacturing and assembly can have just as much impact on the longevity of the BGA connection.  The paragraphs below describe practices which can be used to reduce manufacturing/assembly related problems.

10.1 Solder Wetting Verification

BGA solder balls (tin-lead composition) when in contact with the pads on the PCB will self-align during solder reflow.  However, the ability to visually inspect is limited and non-destructive means will not reveal minute defects in the solder connection.  Therefore, bare PCB wetting verification tests are recommended for each lot of PCB’s to ensure that the PCB surface finish does not inhibit reflow.  It is suggested that an extra coupon be required with each board or panel for this verification test.

10.2. Verification Runs

For mission critical applications, a minimum of three soldering verification runs is recommended for new designs. Verification hardware must be the same parts layout configuration as production hardware; however, equivalent dummy devices may be used in lieu of parts with live die.  Daisy chained parts, when available, should be used to enable electrical verification of completed joints which can not be visually inspected.  Hardware from verification runs should be subjected to visual and oblique angle x-ray inspections and destructive physical analysis.

10.3 Part Moisture Control

Prior to population of flight printed circuit assemblies with PBGA’s or other plastic IC’s, it must be verified that controls for moisture have been followed in accordance with IPC/JEDEC J-STD-033A.  Bake-out of PBGA’s at 125oC for 4 hours is recommended followed by dry storage until use. The time between removal from storage and reflow is dependent upon the parts sensitivity factor per J-STD-033A and must be strictly followed. PCB’s should be baked at 120oC for 3.5 hours.

10.4 Underfill Application

When used, underfill material should be applied following the manufacturer’s recommendations in such a way as to minimize voids. Printed circuit assemblies must be cleaned of flux residues and other contaminants and baked (see 10.3 above) prior to underfill application.

  - X-ray and Visual Inspection

There are numerous limitations that prevent x-ray and visual inspection from being sufficiently thorough inspection methods.  A combination of inspections should be used.  Fiber optic instrumented CCD camera-based inspection systems are available and can enable visual inspection of the inner connections hidden from the outside.  Visual inspection of BGA solder joints may be performed using distal focus endoscopic techniques or equivalent.  X-ray imaging can reveal bridged contacts and voids in the solder balls.  X-ray inspection should be performed using an oblique angle real-time system with at least micron focus capabilities.  Oblique angle transmission can assist in determining the proximity of voids to critical interfaces (solder ball to part and PCB).

11.  Reliability Analysis

Unlike leaded surface mount devices, which have inherent stress relief from lead compliance and where reliability doesn’t vary significantly from device-to-device, many characteristics of the BGA influence the overall reliability. These factors, discussed above, are also summarized in Table 2. Analysis of test data is ongoing to further quantify these sensitivity factors as the primary characteristics that influence overall BGA solder joint reliability. These sensitivity factors are included in reliability modeling software created by Auburn University’s Center for Advanced Vehicle Electronics (CAVE).  The CALCE center at the University of Maryland also has the capability to model BGA interconnect reliability however the sensitivity factors considered in the CALCE product have not been studied for this report.  At the time of this writing, the CAVE statistical modeling tool is available online to CAVE members.  The finite element modeling tool and math model are not available online but are available to CAVE members by contacting CAVE directly at cave@eng.auburn.edu.

| #### Table 2 - Factors that Affect BGA Solder Joint Reliability |  |  |  |
| --- | --- | --- | --- |
| Feature | Lower Reliability | Moderate Reliability | Higher Reliability |
| Part Type | CBGA | CCGA | PBGA |
| Die size to part ratio | Largest |  | Smallest |
| Ball to pad ratio | Smaller |  | Larger |
| Pad type | SMD |  | NSMD |
| Via type | In-pad unfilled | In-pad filled | Interstitial open |
| Via size, min. (aspect ratio) | < 0.020” (> 4:1) |  | ≥ 0.020” (≤ 4:1) |
| Ball size | Smaller |  | Larger |
| Stencil thickness | < 0.006” |  | ≥ 0.006” |
| Underfill | Reworkable UF | No UF | Non-reworkable UF |

Introduction

Since BGA reliability varies significantly with package and assembly architectures, understanding the architecture and inherent reliability is critical to safe implementation of BGA’s in space. This checklist is designed to collect the data needed to adequately analyze the BGA part selection, board design and installation process for suitability for use in space flight hardware.  The analysis may be done using existing expertise (no specific method is detailed herein) or can be done by purchasing the analysis from qualified organizations such as the CAVE center at Auburn University or the CALCE center at the University of Maryland.  The checklist is based upon reference 1 in the list below and reliability test data collected by NASA and the CAVE center.  Additional discussion of the architectural features of BGA’s that influence reliability can be found in the following http://nepp.nasa.gov resources:

1.  Placeholder for Pradeep Lall’s Guidelines document

2.  Ball Grid Array Assembly Reliability, R. Ghaffarian, January 17, 2004, http://nepp.nasa.gov/DocUploads/82697EAD-43DA-41D8-8494322006165BF7/NEPP-webex-present1-17-04A.pdf

3.  Technology Readiness Overview: Ball Grid Array and Chip Scale Packaging, R. Ghaffarian, January 23, 2003, http://nepp.nasa.gov/DocUploads/4D47B29A-4824-4DDD-8A21A4DE4ADADF89/Technology%20Readiness%20Overview%20BGA%20and%20CSP.pdf

4.  Ball Grid Array Reliability Assessment for Aerospace Applications, R. Ghaffarian, Microelectronics Reliability Journal, Volume 39, August 10, 1998, http://nepp.nasa.gov/DocUploads/CD467677-8023-44E3-A795CBCF2DECFF05/RG-MicroRel-1-99.pdf

5.  Shock and Thermal Cycling Synergism Effects on Reliability of CBGA Assemblies, R. Ghaffarian, January 19, 2000, http://nepp.nasa.gov/index_nasa.cfm/619/9A4F59B1-2CC9-46E8-ABED865E68B712AB/

6.  FEA Stress Analysis for the Comparison of BGA and CGA, Mark Fan, September 17, 2001, http://nepp.nasa.gov/index_nasa.cfm/619/36E5103D-EEAC-4E98-80A2FDAB9AAC3EBF/

## Parts Selection

## Internal Design

- What die configuration is used?

Single die

Multiple die (planar orientation)

Multiple die (stacked orientation)

Other:

Rationale:  The configuration of die in the package affects radiation susceptibility, mechanical properties, and thermal mass.

- What is the internal interconnect method employed?

Wire bond

Gold

Aluminum

Other:

Flip chip

TAB

Other:

Rationale:  The internal connection method is often a determining factor in consideration of the absolute amount of thermal energy that can be applied to a package during reflow / rework, the amount of mechanical shock the components can sustain, the potential failure modes, and the reliability of the part to board interconnections.

- What alloy are internal bump terminations (FCP, stack array, etc.)?

Sn05Pb95

Sn03Pb97

Ni/Au

Other:

Not Applicable (wire bond only)

Rationale:  The composition of the internal bump terminations is often a determining factor in consideration of the absolute amount of thermal energy that can be applied to a package during reflow / rework.

- What is the die orientation in the package?

Cavity Up

Cavity Down

Rationale:  The die orientation in the package provides insight about thermal impedance and how to prepare the sample for radiation testing.

- What is the die attach method used?

Elastomeric

Silver-Filled Epoxy

Solder

Other:

Rationale:  The die attach method has an effect on the overall reliability of the die / substrate interconnect, and is often a determining factor in consideration of the absolute amount of thermal energy that can be applied to a package during reflow / rework.

- What is the die size (length, width, thickness)?

Length:       mm  (      in.)

Width:        mm  (      in.)

Thickness:        mm  (      in.)

Rationale:  This information describes the die’s physical attributes.

- What is the die size to package body ratio?

N/A – Multiple die (see “m”)

Ratio:

Rationale:  The die to package ratio influences the thermal coefficient of expansion. The basic assumption is that the die is placed in the approximate center of the package cavity.  Packages with multiple die respond differently. The reliability generally decreases with an increase of the die to package ratio. Packages with smaller die are preferred for applications with excessive thermal cycle exposure.

- What is the die size to array ratio?

N/A – Multiple die (see “m”)

Ratio:

Rationale:  The die to array ratio influences the thermal coefficient of expansion. The basic assumption is that the die is placed in the approximate center of the array pattern.  Packages with multiple die respond differently.

- What are the size and type of the pads on the substrate?

Rationale:   The size of the pads in relation to ball size affects the overall reliability of the solder connection on the package side.  Pad type influences the mechanical strength of the part-side solder joint due to differing solder joint geometries with pad type.

- What is the substrate material and thickness?

Rationale: The substrate material type and thickness affect how the device responds to thermal changes.

How many layers in the substrate?

Layer count:

Unknown

Rationale:  The number of layers in the substrate affects the stiffness of the package and strength of the copper in the vias.

- What type is the substrate (i.e., rigid, flexible)?

Rigid

Flexible

Other:

Rationale:  Flexible substrates are more prone to fatigue damage from thermal excursions.

## External Design

- What is the package material?

Ceramic

Glass-Sealed Ceramic

Metal-Sealed Ceramic

Plastic

Other:

Rationale:  The package material has a direct effect on thermal expansion, thermal dissipation, and radiation susceptibility.

- If plastic, what is the moisture sensitivity level of the device (per J-STD-033) and how has the device been stored?

- Moisture Sensitivity Level and Maximum Exposure Time @  ≤ +30°C / 60% RH

1 – Unlimited (≤ +30°C / 85% RH)

2 – 1 year

2a – 4 weeks

3 – 168 hours

4 – 72 hours

5 – 48 hours

5a – 24 hours

6 – Time specified on Label (TOL)

- Storage

MBB – Vendor

MBB – Repack

Nitrogen-blanket Cabinet

Other:

None

Rationale:  Moisture sensitive components must be stored in Moisture Barrier Bag (MBB) or a controlled environment, such as a drying oven or nitrogen-blanket cabinet to prevent moisture-induced damage.

c.	If plastic, what is the filler content of the mold compound?

Low

High

Rationale: The filler content has an effect on the thermal reliability of a BGA package.

  - What type of termination array pattern does the device employ?

Full Array Populated

Even Row / Even Column

Odd Row / Odd Column

Staggered Pattern

Peripheral Array / Zone Depopulated

Rationale:  Question is describing the termination architecture / pattern, and assists in understanding how the die / chip size interacts with the CTE of the package.

  - Provide the following information concerning the part:

  - Length:        mm /  (      in.)

  - Width:       mm /  (      in.)

  - Thickness including ball/column (prior to reflow):        mm / (      in.)

  - Number of I/O:

  - Pitch:       mm / (      in.)

  - Ball/column diameter (prior to reflow):        mm / (      in.)

  - Ball/column height (prior to reflow):        mm / (      in.)

  - Package side pad surface finish:

Rationale: Defines the package attributes.

  - What is the ball?

In50Pb50

Ni/Au

Sn03Pb97

Sn05Pb95

Sn10Pb90

Sn63Pb36Ag02

Sn63Pb37

Other:

Rationale:  The ball / column alloy is a factor in selecting the reflow temperature and reflow alloy.

  - Does the device employ thermal balls?

--Yes	--No

Rationale:  Devices with thermal balls may require special processing during reflow, and require thermal vias and planes under the device.

## Reliability Assessment

- Has the exact device been thermally cycled in a daisy chained configuration?

Yes

No

Explain:

- Can device reliability be established by similarity to a device that has been tested?

Yes

No

Explain:

- If test data is not available publicly, then a copy of the report or the results should be provided, including the following data:

- Thermal cycle profile/cycles to first failure

- Sample size

- Distribution of failure (e.g., Weibull, log normal)

- If test data was not used, then what method was used to predict reliability of the solder joints?

- What is the CTE and modulus of each material used in the part and are these manufacturer provided or were they determined experimentally?

- If determined experimentally, what method was used (e.g., DMA, TMA)

## PCB and Design Characteristics

- What is the mission / service environment?

--EVA

--Ground Support

--IVA

--Payloads

Rationale:  This question defines the environment and mission.

- What is the expected thermal range and cycles for the useful life of the assembly?

Number of flights required:	-1;	-10;	-100;	-Other:

Estimated thermal cycles per Flight:

Flight Thermal Environment: -      °C to +     °C (-     °F to +     °F)

Board Level Thermal Environment: -      °C to +     °C (-     °F to +     °F)

Maximum thermal swing (Δ°T max):        °C	(      °F)

Rationale:  The mission life and thermal environment drive many of the printed circuit board (PCB) design decisions.  The objective is to base design decisions on realistic mission and thermal profiles, rather than a default flight environment.

- What is the board design type?

Type 1 – Single-sided Board

Type 2 – Double Sided Board

Type 3 – Multilayer board without blind or buried vias

Type 4 – Multilayer board with blind and/or buried vias

Type 5 – Multilayer, metal-core board without blind or buried vias

Type 6 – Multilayer, metal-core board with blind and/or buried vias

Type X – Multilayer with embedded passives (with/without metal-core, with/without blind and/or buried vias)

Type Y – Multilayer with embedded actives (with/without metal-core, with/without blind and/or buried vias)

Rationale:  This question defines the printed circuit board architecture.

- What is the board construction?

Rigid

Flexible

Folded-Flexible

Rigid-Flexible

Rationale:  The type of laminate may define component mounting processes and workmanship requirements.

- What is the board producability level?

A – Simple Through-Hole Technology (THT) only

B – Simple Surface Mount Technology (SMT) only

C – Simple Mixed Technology (SMT / THT)

X – Complex Mixed Technology (SMT / THT / FPT / BGA)

Y – Moderately Complex Mixed Technology (SMT / THT / FPT / BGA / µBGA / UFPT / CSP)

Z – Extremely Complex Mixed Technology (SMT / THT / FPT / BGA / µBGA / UFPT / CSP / TAB / FCP / CIB / COB / Embedded Active / Embedded Passive)

Rationale:  This question defines the technology requirements driving the printed circuit board design.

- What is the printed circuit board laminate and glass transition temperature (Tg)?

BT-Epoxy /

Duroid /

FR4 /

FR5 /

Kapton /

Quartz /

Teflon /

Other:

Rationale:  The choice of laminate is defined by the mission’s environmental requirements, and forces design trade-offs.

- What is the board solderability finish?

Electroplated Gold (Hard)

Electroplated Nickel

ENIG – Electroless Nickel, Immersion Gold

HASL – Hot Air Solder Leveling

I-Ag – Immersion Silver

I-Ni - Immersion Nickel

I-Sn – Immersion Tin

OSP – Organic Solderability Preservative

SMOBC - Solder Mask Over Bare Copper

Wire Bondable Gold (Soft)

Rationale:  The finish processes used to preserve printed circuit board solderability may have an effect on solder assembly processes, overall reliability, and requirement for additional environmental protection (conformal coating).

- What is the expected layer count, internal, and external copper weight?

Number of layers: 	     	Internal weight:	      oz.	External weight:        oz.

Rationale:  Defines printed circuit board construction.

- What is the minimum trace width and spacing?

Trace width:        mm (      in.)	Trace spacing:        mm (      in.)

Rationale:  Trace width and spacing influence produce-ability and workmanship issues.

- What is the printed circuit board finished thickness?

mm /       in.

Rationale:  Finished thickness influences aspects such as thermal expansion coefficient, thermal profile, thermal loading, BGA solder joint reliability, handling, drying, etc.

- What are the number of ground / power planes and the density of traces under the BGA?

Power:       ;	Ground:       ;	Isolation:       ;	Trace Density:       % (relative to full metallization)

Rationale:  The density of metallization under the BGA influences the thermal load required during assembly / rework, thermal dissipation during operation, localized coefficient of expansion, and possible EMI abatement practices.

- How much clearance is there around the BGA(s)?

mm /       in.

Rationale:  Design for Manufacturability (DfM) / Design for Inspectability (DfI) concern.  Sufficient clearance must be provided in the design to allow for inspection, assembly / rework tooling, and to provide a thermal radiation buffer between adjacent components.

- What are the BGA pad sizes, types, and ratio to the ball diameter?

Rationale:  Pad to ball diameter ratio will define the amount of solder paste required, the expected ball-to-pad fillet profile, and the ball-to-pad alignment tolerance / overhang risk.

- Are BGA pads solder-mask defined (SMD)?

--Yes	--No

Rationale:  Solder Mask Defined (SMD) pads can affect ball-to-pad reliability and the ball-to-pad alignment tolerance / overhang risk.

- What type of vias are used and what is the worst case aspect ratio (per device/PCB)?

  - Average aspect ratio:       :1

  - Worst case aspect ratio:       :1

  - Are thermal vias used?

--Yes	--No

  - Are vias in the pads?

--Yes	--No

  - Are vias filled, tented, or plated over?

--Yes	--No

If YES, specify material / process:

If filled:

If tented:

If plated over:

Have materials been tested for outgassing? 	--Yes	--No

Rationale:  These questions address the design and use of vias which have a direct affect on overall assembly reliability.

- Who will be performing micro-section analysis on the printed circuit board coupons?

PCB vendor

Independent certified third party lab

NASA Center Lab

ARC (Ames Research Center)

DFRC (Dryden Flight Research Center)

GRC (Glenn Research Center)

GSFC (Goddard Space Flight Center)

JPL (Jet Propulsion Laboratory)

JSC (Johnson Space Center)

KSC (Kennedy Space Center)

LaRC (Langley Research Center)

MSFC (Marshall Space Flight Center)

SSC (Stennis Space Center)

Rationale:  Coupons shall be included in the printed circuit board build panel and shall comply with IPC-6012 [4.0], Tables 4-1 through 4-4.  Coupon analysis shall comply with IPC Class 3A requirements.  All tested and untested coupons shall be delivered as part of the procurement.

- What is the maximum expected CTE mismatch between the PCB and BGA?

ppm/°C

- What is the CTE mediation method employed?

Compliant layer

Column grid

TAB

Underfill

Other:

- What thermal management method is used for the BGA(s)?

Convection

Forced Convection (Heat sink w/ Fan)

Heat Pump (Recirculating Liquid)

Metal-core PCB

Thermoelectric Module (TEM)

Top-mounted Conduction (Heatsink / Coldplate)

Rationale:  How is the component’s thermal load going to be managed? Use of thermal management processes requires infrastructure planning.

- Will underfill (UF) material be used?

--Yes	--No

If YES, specify material / application process:

Have materials been tested for outgassing? 	--Yes	--No

Rationale:  Prudent use of underfill has been demonstrated to significantly improve the MTBF of solder ball terminations, by a factor of 5X to 10X for fully populated plastic area array packages.  Lack of repair capability must be agreed upon by customer.

## Manufacturing / Quality

- What are the previous experiences with comparable designs with this produce-ability rating?

Rationale:  This question is to allow the vendor to document previous experience with designs of comparable complexity.

- Will any process samples of the printed circuit assembly (PCA) be subjected to DPA prior to approving the assembly process?

--Yes	--No

Explain:

Rationale:  Destructive physical analysis (DPA) of special / unusual terminations may be required to verify effectiveness and reliability.

- How is BGA package warping controlled during reflow?

Rationale:  Warpage of the BGA package during reflow is a known reliability concern.

- What process / verification method is used for ensuring that UF is free of voids or micro-cracks?

- Will C-SAM be employed?

--Yes	--No

Explain:

- Are wetting verification runs required for each bare board?

--Yes	--No

Explain:

- What method will be used to apply solder paste?

Dispensing Process

Automated

Manual

Stencil Process

Laser

Electroformed

Chemical Etch

Screen

Other:

Rationale:  Describes the process used to apply solder paste to the printed circuit board (PCB).

- What size mesh solder solids are to be used for this application?

Mesh size:

Previous experience:

- What type of inspection system is used?

X-ray:	       Define type of x-ray including resolution:

Visual:

Comments:

Rationale:  Defines the type of inspection that will be used. Each type has benefits and limitations.

- Are the ball / column terminations 100% inspected for voids/wetting?

--Yes	--No

Explain:

Rationale:  Defines the level of inspection.

- What criteria are used for determining acceptable level of voiding?

Explain:

- Are the boards cleaned and baked before UF is applied?

--Yes	--No

## Explain: